## Slide 1
The atomic, charge and electronic structure of small Ar cluster ions – an ab initio study
5-th School-Conference on Atomistic Simulation of Functional Materials
J.G. Korobova, A.E Ieshkin, V.S. Chernysh
Moscow State University, Physical Department
e-mail: korobovajg@yandex.ru

## Slide 2
5-th School-Conference on Atomistic Simulation of Functional Materials
Motivation. Why cluster ions?
1
10
102
103
104
105
Atoms
Micro
Macro
Meso
Atom
monomer
dimer
trimer
Bulk region
Micro
clusters
Small
clusters
Large
clusters
Nanoclusters
cluster ion assisted deposition of films
Ion implantation

## Slide 3
5-th School-Conference on Atomistic Simulation of Functional Materials
Objective
Cluster ion atomic and charge structure affects the interaction between cluster ion and irradiated surface
FCC structure
Isosahedrical structure
Aim: to obtain charge distribution in Ar+ cluster ions
Methodology:
DFT – supercell approach,
Plane wave basis set
Local Density Approximation (LDA)
Spin-orbital coupling
Considered cluster sizes:
Ar13
Ar19
Ar55
Ar135

## Slide 4
5-th School-Conference on Atomistic Simulation of Functional Materials
Neutral Ar clusters
Cluster | Efcc – Eisp, meV
13 | 61.04807
19 | 38.10684
55 | 164.867
135 | -
fcc
Atomic structure and stability
isp
Ar13
Ar55
Isosahedrical structure is more preferable

## Slide 5
5-th School-Conference on Atomistic Simulation of Functional Materials
Ar+ cluster ions
Cluster | Minimal interatomic distance, Å | 
 | Ar0 | Ar+
Ar13 fcc | 3.46 | 3.38
Ar13 isp | 3.38 | 3.30
Ar19 fcc | 3.48 | 3.47
Ar19 isp | 3.35 | 3.33
Ar55 fcc | 3.72 | 3.44
Ar55 isp | 3.32 | 3.30
Ar135 fcc | 3.48 | 3.46; 3.44
Cluster | E(Ar+) – E(Ar0), meV |  | μ(Ar+), μB | 
 | Fcc | isp | fcc | isp
13 | 11.4 | 11.4 | 0.85 | 0.85
19 | 10.6 | 10.7 | 0.86 | 0.87
55 | 10.4 | 10.4 | 0.86 | 0.87
135 | 9.8 21.3 |  | 0.86 1.73 | 
Atomic structure and stability
Isosahedrical structure is still more preferable
Neutral cluster is more stable
Cluster ion is more close packed
Cluster ion has magnetic moment

## Slide 6
5-th School-Conference on Atomistic Simulation of Functional Materials
Ar+ cluster ions
Distribution of charge difference between Ar0 and Ar+
fcc
isp
Ar13
Ar55
Ar135
Ar+
Ar+2
(111)
(001)

## Slide 7
5-th School-Conference on Atomistic Simulation of Functional Materials
Ar+ cluster ions
Electronic structure
fcc
isp
Ar13