## Slide 1: THEORETICAL INVESTIGATION OF TRANSITION METAL BASED QUASI-TWO-DIMENSIONAL STRUCTURES
Authors:
Konstantin V. Larionov Dmitry G. Kvashnin Pavel B. Sorokin
7-th School-Conference on Atomistic Simulation of Functional Materials (ASFM 2018)
Photochemistry Center,
September 12–13, 2018

## Slide 2
A very small introduction
Outline
Theoretically-experimental investigation of 2D copper oxide (CuO) with uncommon square lattice structure
Prediction of a new 2D phase of iron oxide (FeO) and investigation of its heterojunctions with graphene
Prediction of a new 2D phase of cobalt oxide (CoC) and investigation of its properties
Some conclusion remarks

## Slide 3
Двумерные гетеросоединения на основе графена
Liu Z. et al.
In-plane heterostructures of graphene and hexagonal boron nitride with controlled domain sizes // Nature Nanotechnology. 2013.
a
b
Zhao J. et al.
Free-Standing Single-Atom-Thick Iron Membranes Suspended in Graphene Pores // Science. 2014.
c
d
Two-dimensional materials
Lee J. et al.
Tunable Lattice Constant and Band Gap of Single- and Few-Layer ZnO // The Journal of Physical Chemistry Letters. 2016.
e
f

## Slide 4
ADF-STEM image of the Cu cluster and atoms on graphene sheet.
Beam-shower technique as room temperature was used to prevent both contamination and aggregation of Cu atoms.
Sharp threshold peaks indicate a partial emptying of the Cu 3d band caused by the chemical bond with oxygen.
1 nm
2-Cu
1-Cu
1-G
None
Experimental observation of 2D CuO on graphene
Kano E. et al. One-Atom-Thick 2D Copper Oxide Clusters on Graphene. Nanoscale 2017, 9 (11), 3980–3985.

## Slide 5
Based on experimental results, the model of 2D Cu cluster on graphene surface with the same size was constructed.
STEM image simulation totally confirmed the experimental observations
The oxygen impurity atoms placed in the centers of Cu rectangles play the major role in the stabilization of orthogonal lattice of 2D Cu.
With the absence of oxygen impurities the 2D Cu cluster tends to curve, form 3D structure and bind with the graphene surface.
1
Exp.
Simul.
Modeling of Cu-based cluster on graphene

## Slide 6
2D CuO is a wide gap semiconductor with Eg = 2.5 eV, while bulk CuO has a band gap about 1.5 eV.
Unlike the bulk phase of Cu and CuO which have a paramagnetic (PM) ground state, the 2D CuO has a weak antiferromagnetic (AFM) ground state with the energy difference between PM and AFM about ~ –0.18 meV/atom.
Y
Electronic and magnetic properties of 2D CuO
Kano E. et al. One-Atom-Thick 2D Copper Oxide Clusters on Graphene. Nanoscale 2017, 9 (11), 3980–3985.

## Slide 7
E, eV/FeO
-14.3
-14.2
1
2
3
4
“Ionic graphitization” effect in ultrathin FeO films
Rocksalt FeO film (111)
d
-2.0
-1.5
-1.0
-0.5
0.0
0.5
1.0
1
2
3
4
5
6
7
8
9
10
11
12
Number of layers, N
ΔE, eV/FeO
Step
3.1 Å
Stack of 2D FeO (001)
~ 0.1 eV/FeO

## Slide 8
Elastic constant | C (N/m)
FeO(ZZ1), C11 | 150
FeO(ZZ2), C22 | 137
FeO, C12 | 57
FeO, C66 | 27
Properties of 2D FeO
Graphene, C11 = 367 N/m
MoS2, C11 = 140 N/m
АFM2
E = -14.33 eV/FeO
FM
E = -14.22 eV/FeO
NM
E = -12.57 eV/FeO
d1 = 2.80 Å
d2 = 2.76 Å
= AFM - NM
= -1.7 eV/FeO
= -1.5 eV/FeO
Larionov K. et al. The Journal of Physical Chemistry C 2018, 122 (30), 17389–17394.

## Slide 9
2D FeO stability
Larionov K. et al. The Journal of Physical Chemistry C 2018, 122 (30), 17389–17394.

## Slide 10
ЗАГОЛОВОК СЛАЙДА
[1]
[2]
ZZ+ZZ(Fe)
ZZ+ZZ(O)
AC+ZZ(Fe)
AC+LN
ZZ+LN
AC+ZZ(O)
[1] Liu et al. Nano Lett. 2011
[2] Liu et al. Physical Review Letters 2010
Investigation of 2D FeO/graphene interface
linear (LN)
zigzag (ZZ)

## Slide 11
Determination of equilibrium shape of FeO film in graphene pore
Concentrations of iron and oxygen atoms are not equal in case of ZZ edge. Thus, one should take into account a difference of their chemical potentials:
Larionov K. et al. The Journal of Physical Chemistry C 2018, 122 (30), 17389–17394.

## Slide 12
Simulation of 2D FeO film in graphene nanopore
a, b, d) Larionov K. et al. The Journal of Physical Chemistry C 2018, 122 (30), 17389–17394.
c) Zhao J. et al. Science 2014, 343 (6176), 1228–1232.

## Slide 13
2D CoC of different lattice type
Larionov K. et al. Study of the New Two-Dimensional Compound CoC. JETP Letters 2018, 108 (1), 13–17

## Slide 14
MD and bending analysis of o-CoC stability
Chart: 1/d2, 1/Å2
| 0 | 1.479981766624635E-2 | 1.7825280168841051E-2 | 2.3415790086808184E-2 | 3.1492864110653329E-2 | 4.5559695160079697E-2
 | 0 | 0.02833 | 0.036378 | 0.048345 | 0.066005 | 0.091273

## Slide 15
Electronic and mechanical properties of o-CoC
C11 (N/m) | 229
C12 (N/m) | 71
C22 (N/m) | 241
C66 (N/m) | 68
ν12 | 0.31
ν21 | 0.29
D1 (eV) | 1.23
D2 (eV) | 1.63
Larionov K. et al. Study of the New Two-Dimensional Compound CoC. JETP Letters 2018, 108 (1), 13–17
Graphene, C11 = 367 N/m
MoS2, C11 = 140 N/m
Graphene, D = 1.46 eV

## Slide 16
Conclusion
  So, to be continued…
2D CuO
  Orthorhombic structure
  Semiconducting and antiferromagnetic properties
  Experimentally observed
  2D FeO
  Orthorhombic structure
  Semiconducting and strong antiferromagnetic properties
Seems to be experimentally observed
  2D CoC
  Orthorhombic structure
  Metallic and prospective mechanical properties
  No evidence of experimental observation. Yet.

## Slide 17: Acknowledgments
Pavel B. Sorokin Dmitry G. Kvashnin Zakhar I. Popov
Research Laboratory of Theoretical Modeling of New Materials, TISNCM, Troitsk, Moscow
Join us via www.facebook.com/SorokinTheorGroup/
Head of theoretical group: Dr. habil. Pavel B. Sorokin
Research Laboratory “Inorganic Nanomaterials”, NUST MISIS, Moscow

## Slide 18
!

## Slide 19
,
–2D FeO monolayer energy per FeO unit;
,
–2D FeO monolayer energy per FeO unit;
– number of “extra-atoms” (Fe or O, blue dashed)
Determination of equilibrium shape of FeO film in graphene pore

## Slide 20
Ссылки на свои статьи
Тезисно выводы по каждому слайду
Анимации к слайдам. Да побольше 
Анимации к MD и FeO(hex -> square)
Благодарности
Нормальный Outline
  Systematic investigation of two-dimensional transition metal oxides and carbides as well as hetererostructures based on them is of great interest because of their high promising electronic and magnetic properties appearing at the low dimension.

## Slide 21
Fan, D.; Lu, S.; Hu, X. Two-Dimensional Iron Monocarbide with Planar Hypercoordinate Iron and Carbon.
arXiv:1802.03673 [cond-mat.mtrl-sci]

## Slide 22
2D-CuO
  Formation of CuO monolayers with square lattice was predicted and found to be in agreement with STEM/EELS experiments
  Semiconducting and weak antiferromagnetic properties of 2D-CuO were shown
  2D-FeO
“Ionic graphitization” of ultrathin rocksalt FeO films into stack of monolayers with orthorhombic lattice type and strong antiferromagnetic ordering was shown
2D-FeO/graphene interface energy and its shape under external conditions were described analytically
Possibility of experimental observation of 2D-FeO was proposed
  2D-CoC
  New 2D phase of CoC with orthorhombic lattice was proposed and its prospective stability was shown
  Mechanical and electronic properties analysis of o-CoC was carried out
Summary