## Slide 1
T.I. Burganov,*1
S.A. Katsyuba,1 T.P. Gerasimova,1 S.M. Sharipova,1 A.A. Kalinin,1 A. Monari,2 X. Assfeld.2
1 Arbuzov Institute of Organic and Physical Chemistry, FRC Kazan Scientific Center of RAS, Kazan, Russia
2 University of Lorraine, Laboratory of theoretical chemistry and physics, CS 25233, Nancy, France
* e-mail: timk90@mail.rua
Novel push-pull quinoxalinone-based chromophores with high sensitivity of emission and absorption
to small structural modifications
Moscow 2018
7-th School-Conference on Atomistic
Simulation of Functional Materials
(ASFM 2018)

## Slide 2
π
D
А
Nonlinear optics
(NLO - materials)
Organic solar cells (DSSCs/BHJ)
Organic light-emitting diodes (OLEDs)
Donor – π – Acceptor
systems
Luminescent sensors
Applications of push-pull systems

## Slide 3
Considered quinoxalinone-based D/A-π-A compounds
π
D
А
π
A
А
3

## Slide 4
Experimental photophysical
properties
4

## Slide 5
Positive solvatochromic
behavior
Compound 1 |  |  |  |  |  | 
 | dioxane | Ethyl Acetate | CH2Cl2 | Acetone | CH3CN | DMSO
λmax, nm | 354 | 354 | 362 | 359 | 359 | 367
eV | 3.50 | 3.50 | 3.43 | 3.45 | 3.45 | 3.38
ε | 26500 | 23454 | 46000 | 41589 | 44000 | 30432
λemi, nm | 523 | 550 | 590 | 598 | 610 | 616
eV | 2.37 | 2.25 | 2.10 | 2.07 | 2.03 | 2.01
φ | 0.13 | 0.05 | 0.023 | 0.003 | <0.01 | <0.01
Stokes shifts |  |  |  |  |  | 
Δλemi, nm | 169 | 196 | 228 | 239 | 251 | 249
eV | 1.13 | 1.25 | 1.32 | 1.38 | 1.42 | 1.37
Δν,cm-1 | 9128 | 10067 | 10675 | 11133 | 11462 | 11014
Absorption
Emission
5

## Slide 6
Calculated electronic transitions on optimized S0
with PBE0/def2-TZVP
ΔGB-A < 0.2 kcal/mol
6

## Slide 7
Calculated NTO for the first electronic transitions on optimized S0
with PBE0/def2-TZVP
Occupied NTO
Virtual NTO
1st
2d
Partialy
ICT
ϕS = 0.71
ϕS = 0.91
Local
π→π*
ICT – intramolecular charge transfer
7

## Slide 8
Calculated electronic transitions on optimized S0
with PBE0/def2-TZVP
Experiment |  | Calculations |  |  |  | 
λmax, nm/eV | λemi, nm/eV | S0→Sn, nm/eV (f) | S1→S0, nm/eV (f) | Nature of S0→S1 (ϕS) | μ(S0), D | ΔE (ΔG) kcal/mol
DIOX 362/ 3.43 DCM 363/ 3.43 | DIOX 523/ 2.37 DCM 590/ 2.10 | GAS S0→S1 406/ 3.05 (0.03) S0→S2 357/ 3.47 (1.48) | GAS 507/ 2.45 (0.049) DCM(PCM) 550/ 2.26 (0.143) | Local with partial CT (0.71) S0→S2 Local π→π* (0.91) | 5.93 | 0.14 (0.13)
Calculated and Experimental Emission
Calculated and Experimental Absorption
8

## Slide 9
Experimental photophysical properties
9

## Slide 10
NTO for the first electronic transitions of 2 and 3
1st
1st
Partial ICT
More local
than 1
ϕS = 0.72
ϕS = 0.68
ICT – intramolecular charge transfer
Occupied NTO
Virtual NTO
Partial ICT
More local
than 1
10

## Slide 11
 | Experiment |  | Calculations |  |  |  | 
 | λmax, nm/eV | λemi, nm/eV | S0→S1, nm/eV (f) [d] | S1→S0, nm/eV (f) [d] | Assignment for S0→S1 (ϕS) | μ(S0)D | ΔE, (ΔG) kcal/mol
1 | DCM 362/ 3.43 | DCM 590/ 2.10 | 406/3.05 (0.03) S0→S2 357/3.47 (1.48) | DCM 550/ 2.26 (0.143) | Local with partial CT (0.71) S0→S2 π→π* (0.91) | 5.93 | 0.14 (0.13)
2 | DIOX 442/ 2.81 DCM 447/ 2.77 | DIOX 530/ 2.34 DCM 560/ 2.21 | GAS 433/ 2.86 (1.17) | GAS 478/ 2.60 (1.627) DCM(PCM) 564/ 2.20 (1.533) | Local with partial CT π→π* (0.72) | 1.95 | 0.76 (1.07)
3 | DIOX 397/ 3.08 DCM 403/ 2.22 | DIOX 497/ 2.49 DCM 558/ 2.21 | GAS 409/ 3.03 (1.07) | GAS 448/ 2.76 (1.16) DCM(PCM) 532/ 2.33 (1.556) | Local with partial CT π→π* (0.68) | 7.70 | 0.06 (0.08)
11

## Slide 12
Occupied NTO
Virtual NTO
 | Experiment In DCM |  | Calculations with TDDFT (PBE0/def2-TZVP) gas/PCM(DCM) |  | 
 | λmax, nm/ eV | λemi, nm/ eV | S0→S1, nm/eV (f) [d] | S1→S0, nm/eV (f) /PCM in bold | ΔE[c], (ΔG) kcal/ mol
2 | 447/ 2.77 | 560/2.21 | 433/2.86 (1.17) | 478/2.60 (1.627) 564/2.20 (1.533) | 0.76 (1.07)
4 | 462/2.68 | 580/2.14 | 431/2.88 (1.27) | 469/2.64 (1.19) 550/2.26 (1.740) | 0.81 (1.08)
12

## Slide 13
Linear correlation between ET(30) values and the experimental positions of λemi
13

## Slide 14
Rotamer A
(major)
Rotamer B
(minor)
ΔGA-B =
3.7 kcal/mol
 | Experiment In DCM |  | Calculations with TDDFT (PBE0/def2-TZVP) gas/PCM(DCM) |  | 
 | λmax, nm/ eV | λemi, nm/ eV | S0→S1, nm/eV (f) [d] | S1→S0, nm/eV (f) /PCM in bold | ΔE[c], (ΔG) kcal/ mol
1 | 362/ 3.43 | 590/ 2.10 | 406/ 3.05 (0.03) S0→S2 357/ 3.47 (1.48) | 507/ 2.45 (0.049) 550/ 2.26 (0.143) | 0.14 (0.13)
5 | DIOX 441/ 2.81 DCM 452/ 2.74 | DIOX 526/ 2.36 DCM 537/ 2.31 | GAS 431/ 2.88 (0.26) | GAS 501/ 2.48 (0.1726) DCM(PCM) 555/2.24 (0.3638) | 4.35 (3.69)
14

## Slide 15
 | Experiment In DCM |  | Calculations with TDDFT (PBE0/def2-TZVP) gas/PCM(DCM) |  | 
 | λmax, nm/ eV | λemi, nm/ eV | S0→S1, nm/eV (f) [d] | S1→S0, nm/eV (f) /PCM in bold | ΔE[c], (ΔG) kcal/ mol
1 | 362/3.43 | 590/2.10 | 406/ 3.05 (0.03) S0→S2 357/ 3.47 (1.48) | 507/ 2.45 (0.049) 550/ 2.26 (0.143) | 0.14 (0.13)
5 | 450/2.76 | 526/2.36 | 431/ 2.88 (0.26) | 501/ 2.48 (0.1726) 555/ 2.24 (0.3638) | 4.35 (3.69)
6 | DIOX 462/ 2.68 DCM 469/2.64 | DIOX 590/ 2.10 DCM 606/2.05 | GAS 490/ 2.53 (0.87) | GAS 574/ 2.16 (0.9222) DCM(PCM) 633/ 1.96 (1.3160) | 1.33 (1.51)
rotamer B
(0 kcal/mol)
rotamer A
(1.0 kcal/mol)
rotamer C
(1.3 kcal/mol)
rotamer D
(2.2 kcal/mol)
15

## Slide 16
1st
Purely
local π→π*
1st
ϕS = 0.71
ϕS = 0.79
Purely
local π→π*
Occupied NTO
Virtual NTO
NTO for the first electronic transitions of 5 and 6
16

## Slide 17
Conclusions
The capacity of a series of novel push-pull quinoxalinone based chromophores to absorb and emit radiation in the broad range of visible spectrum is demonstrated. Their absorption and emission are shown to depend dramatically on quite moderate structural modification of the molecules.
Quantum-chemical calculations within TDDFT approach using cost-effective PBE0/def2-TZVP method with PCM model reasonably reproduce main spectral features and trends along with solvatochromic behavior.
Seemingly gigantic Stokes Shift of 1 has been explained on the basis of the calculations
The moderate charge-transfer character established for all the systems using NTO and detachment/attachment density matrices is shown to be non the main factor affecting the photophysical properties
No dependence of the photophysical characteristics of the chromophores on the conformation of the DMAS group is found.
For more details:
Burganov T. I., et al, Physical Chemistry Chemical Physics., 2018, 20, 21515-21527. https://pubs.rsc.org/en/content/articlelanding/2018/cp/c8cp03780a#!divAbstract
17

## Slide 18
Acknowledgements
The reported study was funded by RFBR according to the research project
№ 18-33-00128 mol_a
TB gratefully acknowledges researcher-mobility funding program of the government of the Republic of Tatarstan “Algarysh-2017”
(grant №12440 24.05.17)
Special thanks are due to Prof. L. Zakharova and Dr. D. Gabdrakhmanov for their kind assistance in fluorimetric measurements.
18

## Slide 19
Thank you for your kind attention

## Slide 20
20

## Slide 21
1 | 2 | 3 | 4 | 5 | 6
Acetone |  |  |  |  | 
359 | 441 | 397 | 455 | 448 | 466
3.45 | 2.81 | 3.12 | 2.72 | 2.77 | 2.66
41589 | 28730 | 36336 | 32186 | 8600 | 11300
598 | 572 | 583 | 599 | 560 | 635
2.07 | 2.17 | 2.13 | 2.07 | 2.21 | 1.95
0.003 | 0.17 | 0.53 | 0.23 | 0.08 | 0.02
CH3CN |  |  |  |  | 
359 | 439 | 397 | 453 | 450 | 467
3.45 | 2.82 | 3.12 | 2.74 | 2.76 | 2.65
44000 | 26000 | 33000 | 32500 | 10500 | 9200
610 | 588 | 609 | 611 | 561 | 635
2.03 | 2.11 | 2.04 | 2.03 | 2.21 | 1.95
<0.01 | 0.16 | 0.03 | 0.13 | 0.06 | 0.03
DMSO |  |  |  |  | 
367 | 454 | 407 | 466 | 452 | 470
3.38 | 2.73 | 3.05 | 2.66 | 2.74 | 2.64
30432 | 30993 | 32459 | 31062 | 9800 | 18500
616 | 602 | 619 | 624 | 580 | 655
2.01 | 2.06 | 2.00 | 1.99 | 2.14 | 1.89
<0.01 | 0.28 | 0.11 | 0.19 | 0.02 | 0.03
 | 1 | 2 | 3 | 4 | 5 | 6
 | 1,4-dioxane |  |  |  |  | 
λmax, nm | 354 | 442 | 397 | 457 | 441 | 462
eV | 3.50 | 2.81 | 3.12 | 2.71 | 2.81 | 2.68
ε | 26500 | 31000 | 33000 | 26000 | 9500 | 19600
λemi, nm | 523 | 530 | 497 | 556 | 525 | 590
eV | 2.37 | 2.34 | 2.49 | 2.23 | 2.36 | 2.10
φ | 0.13 | 0.11 | 0.81 | 0.16 | 0.05 | <0.01
 | Ethyl Acetate |  |  |  |  | 
λmax, nm | 354 | 439 | 394 | 453 | 445 | 460
eV | 3.50 | 2.82 | 3.15 | 2.74 | 2.79 | 2.70
ε | 23454 | 25850 | 30482 | 27816 | 12500 | 25000
λemi, nm | 550 | 544 | 527 | 569 | 538 | 610
eV | 2.25 | 2.28 | 2.35 | 2.18 | 2.30 | 2.03
φ | 0.05 | 0.12 | 0.80 | 0.20 | 0.08 | 0.03
 | CH2Cl2 |  |  |  |  | 
λmax, nm | 362 | 446 | 403 | 464 | 452 | 469
eV | 3.43 | 2.78 | 3.08 | 2.67 | 2.74 | 2.64
ε | 46000 | 39000 | 25500 | 24000 | 11000 | 10600
λemi, nm | 590 | 561 | 558 | 581 | 537 | 606
eV | 2.10 | 2.21 | 2.22 | 2.13 | 2.31 | 2.05
φ | 0.023 | 0.15 | 0.62 | 0.17 | 0.05 | 0.04

## Slide 22
 | 1 | 2 |  | 3 | 4 | 5 | 6
Stokes shifts |  |  |  |  |  |  | 
 | 1,4-dioxane |  |  |  |  |  | 
Δλemi, nm | 169 | 88 | 100 |  | 99 | 84 | 128
eV | 1.13 | 0.47 | 0.63 |  | 0.48 | 0.45 | 0.58
Δν,cm-1 | 9128 | 3757 | 5068 |  | 3896 | 3628 | 4696
 | Ethyl Acetate |  |  |  |  |  | 
Δλemi, nm | 196 | 105 | 133 |  | 116 | 93 | 150
/eV | 1.25 | 0.55 | 0.79 |  | 0.56 | 0.48 | 0.66
Δν,cm-1 | 10067 | 4397 | 6405 |  | 4500 | 3885 | 5346
 | CH2Cl2 |  |  |  |  |  | 
Δλemi, nm | 228 | 115 | 155 |  | 117 | 85 | 137
/eV | 1.32 | 0.57 | 0.85 |  | 0.54 | 0.43 | 0.60
Δν,cm-1 | 10675 | 4596 | 6893 |  | 4340 | 3502 | 4820
 | Acetone |  |  |  |  |  | 
Δλemi, nm | 239 | 131 | 186 |  | 144 | 112 | 169
/eV | 1.38 | 0.64 | 1.00 |  | 0.66 | 0.55 | 0.71
Δν,cm-1 | 11133 | 5193 | 8036 |  | 5284 | 4500 | 5700
 | CH3CN |  |  |  |  |  | 
Δλemi, nm | 251 | 149 | 212 |  | 158 | 111 | 168
/eV | 1.42 | 0.72 | 1.09 |  | 0.71 | 0.55 | 0.70
Δν,cm-1 | 11462 | 5772 | 8769 |  | 5709 | 4397 | 5665
 | DMSO |  |  |  |  |  | 
Δλemi, nm | 249 | 148 | 212 |  | 158 | 128 | 185
/eV | 1.37 | 0.67 | 1.04 |  | 0.67 | 0.61 | 0.75
Δν,cm-1 | 11014 | 5415 | 8415 |  | 5434 | 4883 | 6010
22