## Slide 1: Исследование структуры Si(111) поверхности, терминированной атомами H, метиловыми, этиниловыми и пропиниловыми группами
E. Heifets
Max Planck Institute for Solid State Research, Stuttgart, Germany

## Slide 2
MOTIVATION
Semiconductor (Si) surface passivation;
Oxidation resistance of semiconductor surface;
Interfaces of semiconductors with organic, polimer and biological materials:
  Structure;
  Electric properties of passivated semiconductor surface;
  Electric fields appearing at the interfaces;
  Charge transfer across such interfaces/contacts;
  Energy transfer across such interfaces/contacts;
Functionalization of semiconductor surfaces for:
  Photoelectrochemical devices for fuel and energy production, including photo-electrolyze of water;
  Molecular electronics;
  Sensors;
  Interfaces (contacts) of organic phosphorous materials with semiconductors.

## Slide 3
Computational details
CRYSTAL14 code: Local Gaussian type basis set
Gaussian Basis Sets of Triple-Zeta Valence with Polarization Quality for Solid-State Calculations (pob_TZVP_2012 ),
Journal of Computational Chemistry 2012, DOI: 10.1002/jcc.23153
Hybrid density functional: B3PW
8x8x1 Monkhorst-Pack net

## Slide 4
-H | -CH3 | -C≡C-H | -C≡C-CH3
12 layer Si [111] slab with different adsorbates:

## Slide 5
1.487 Å
0.789Å (+1.51%)
2.327Å (-0.21%)
0.776Å (-0.22%)
2.331Å (-0.06%)
+0.007e
+0.188e
-0.194e
-0.006e
+0.005e
0.000e
charges
distances
12 layer Si [111] slab with adsorbed –H
+0.007e

## Slide 6
12 layer Si [111] slab with adsorbed –CH3
1.328 Å (-0.19%)
0.775Å (-0.33%)
2.331Å (-0.03%)
0.777Å (-0.03%)
2.332Å (-0.01%)
distances
0.805Å (+3.55%)
1.893 Å
0.387 Å
-0.152e
-0.004e
+0.004e
0.000e
0.000e
0.000e
charges
+0.257e
-0.335e
+0.077e
110.82°
5.81°
dC-H= 1.089 Å
-0.104e

## Slide 7
1.806 Å
0.794Å (+2.19%)
2.331Å (-0.03%)
0.777Å (-0.04%)
2.331Å (-0.05%)
distances
-0.121e
+0.287e
-0.161e
-0.020e
+0.010e
0.001e
charges
1.198 Å
1.061 Å
-0.041e
+0.046e
12 layer Si [111] slab with adsorbed –C≡C-H
-0.116e

## Slide 8
12 layer Si [111] slab with adsorbed –C≡C-CH3
2.331 Å (-0.03%)
0.777Å (-0.03%)
2.331Å (-0.04%)
0.777Å (-0.04%)
2.332Å (-0.01%)
distances
1.201 Å
1.440Å
+0.284e
-0.020e
+0.010e
+0.001e
0.000e
0.000e
charges
-0.122e
+0.026e
-0.153e
0.54°
1.804 Å
0.795Å (+2.28%)
0.403Å
-0.159e
-0.117e
dC-H= 1.093 Å
111.61°
+0.044e

## Slide 9
1s-Si DOSSs for 12 layer Si [111] slab:
comparison for different adsorbates
-H
-CH3
-C≡C-H
-C≡C-CH3

## Slide 10
1s-Si DOSSs for 12 layer Si [111] slab:
comparison for different adsorbates
 | -H | -CH3 | -C≡C-H | -C≡C-CH3
Si1-Si2 | -0.047 | -0.217 | -0.345 | -0.349
Si2-Si3 | 0.109 | 0.219 | 0.180 | 0.181

## Slide 11
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -H

## Slide 12
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -H

## Slide 13
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -CH3

## Slide 14
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -CH3

## Slide 15
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -C≡C-H

## Slide 16
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -C≡C-H

## Slide 17
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -C≡C-CH3

## Slide 18
Valence band structure and total DOSS for Si [111] 12 layer slab with adsorbed -C≡C-CH3

## Slide 19
 | ΔEg(Γ-Γ) | ΔEg(M-M) | ΔEg(K-K) | ΔEg(M-Γ)
-H | 2.95 | 3.71 | 5.50 | 2.44
-CH3 | 2.91 | 3.67 | 5.42 | 2.42
-C≡C-H | 2.90 | 3.52 | 4.94 | 2.39
-C≡C-CH3 | 2.90 | 3.50 | 4.90 | 2.38
Comparison of band gaps
for different adsorbates at Si [111] 12 layer slab
Si bulk:
Exp. ΔEg= 1.15 eV (CRC Handbook Phys. And Chem. )
1.14 eV (Streetman, Ben G.; Sanjay Banerjee (2000). Solid State electronic Devices (5th ed.). New Jersey: Prentice Hall. p. 524.)
Calc. ΔEg= 2.06 eV

## Slide 20
Distances between two surface layers in Si slab increased (by 1.5-3.5%). All other distances between layers in the modeled slabs decreased, but by very small value.
There is an electron density transfer from the top surface layer of Si slab to the subsurface layer and to considered adsorbates. In the case of -H adsorption the density transfer to the adsorbate is negligible. Then it grows at –CH3 and more at –C≡C-H and –C ≡ C-CH3 .
The charges of subsurface Si atoms are significant and negative. This cases attraction of positively charged H atoms in -CH3 groups and appropriate rotation of these groups.
Band bent near Si [111] surface is nonmonotonic: it bends up at the subsurface layer, then down at the surface layer of the surface. The band bent is limited to two surface layers.
The electrons located at the subsurface layer of Si [111] surface have the largest one-electron energy.
Electron states located at adsorbate and at surface Si layer are submerged into valence and conduction bands. The band edges are defined by electrons located at subsurface Si.
Summary:

## Slide 21
Thank you for your attention!