## Slide 1
Alexander Kvashnin
Computational search for new
superhard transition metal borides
13.09.2018, Moscow
Atomistic Simulation of Functional Materials» (ASFM-2018 Fall)

## Slide 2
Outline
Introduction + Motivation
Methods
Superhard Cr-based materials
Prediction and synthesis of new WB5
Study of Mo-B system

## Slide 3: Introduction
Science 245, 841 (1989)
B4C
~98 GPa
~60 GPa
Transition metal borides and carbides
Phys. Chem. Chem. Phys., 2016,18, 2361
Diamond
c-BN
~92 GPa
~32 GPa
~50 GPa

## Slide 4: Why it is important?
PCD, c-BN,
Mixture PCD/BN
Ease in synthesis and production
These materials have high melting temperature
High hardness allows them to be used in many other different fields of technology
Possible applications:
Manufacturing industry
Mining industry
Hard alloys of
WC, TiN etc.
Substitution of traditional materials

## Slide 5: Methods
Computational search for new materials was carried out using the evolutionary crystal structure prediction algorithm USPEX
Geometry relaxation and calculations of mechanical properties were performed at a density functional level of theory using PBE parameterization implemented into VASP package

## Slide 6
Natoms | Variants | CPU time
1 | 1 | 1 sec.
10 | 1011 | 103 yrs.
20 | 1025 | 1017 yrs.
30 | 1039 | 1031 yrs.
Overview USPEX
(Oganov & Glass,
J.Chem.Phys. 2006)
Need to find GLOBAL energy minimum.
Trying all structures is impossible:
Notes: «Нет», если бы это слово было полным содержанием данной статьи, первой в химической литературе статьи, состоящей из одного слова, то этим можно было бы достаточно надежно охарактеризовать состояние данной области.

## Slide 7: USPEX project (Universal Structure Prediction: Evolutionary Xtallography)
http://uspex-team.org
The most popular code for computational materials design in the world (>4300 users from 78 countries).
Effort of ~80 man-years.
>400 publications, 5 patents.
Universal:
-prediction of stable structure AND composition, 3D, 2D, 1D, 0D – systems.
-optimization of physical properties,
-prediction of phase transition mechanisms

## Slide 8: USPEX project (Universal Structure Prediction: Evolutionary Xtallography)
(Random) initial population
Evaluate structures by relaxed (free) energy
Select lowest-energy structures as parents for new generation
Standard variation operators:
(1) Heredity (crossover)
(2) Lattice mutation
(3) Permutation
+(4) Transmutation +(5) Rotational mutation +(6) Soft-mode mutation +...

## Slide 9: Automatic search for ground states in multicomponent system
Thermodynamic stability in variable-composition systems
Stable structure must be below all the possible decomposition lines !!
Example of a ternary system
A B
AB
AB5
Convex Hull

## Slide 10: Search for new phases in Cr-B, Cr-C, Cr-N systems

## Slide 11: Search for new phases in Cr-B , Cr-C, Cr-N systems
New phase, has not been studied before
Superhard material with Hv ~50 GPa
High energy density materials

## Slide 12: W-B system
A.G. Kvashnin, et al., J. Phys. Chem. Lett., 2018, 9, pp 3470–3477
Vickers hardness of WB5 is 45 GPa

## Slide 13: Temperature stability
[x] J. Phase Equilibria 1995, 16 (2), 150–161
[o] Sov. Powder Metall. Met. Ceram. 1974, 13 (1), 1–3
A.G. Kvashnin, et al., J. Phys. Chem. Lett., 2018, 9, pp 3470–3477

## Slide 14: Temperature dependence of mechanical properties
A.G. Kvashnin, et al., J. Phys. Chem. Lett., 2018, 9, pp 3470–3477

## Slide 15: Hardness vs Fracture toughness
Ashby plot may show the material with optimal combination of Vickers hardness and fracture toughness.
WB5 is new optimal material
A.G. Kvashnin, et al., J. Phys. Chem. Lett., 2018, 9, pp 3470–3477

## Slide 16: Hardness vs Fracture toughness
Samples of new superhard material
Measurements of hardness and fracture toughness
ВК6 (WC+6Co)
WB5
ВК6 (WC+6Co)
WB5

## Slide 17: Mo-B system
A.G. Kvashnin, et al., Submitted 2018
New MoB5 is stable in the entire temperature range
MoB4 is metastable.
MoB5 has lower hardness compared to WB5

## Slide 18: Dependence of mechanical properties on the doping
A.G. Kvashnin, et al., Submitted 2018
M10.9M20.1B5
M1 = W,Mo
M2 = Ti,V,Cr,Zr,Nb,Mo,Hf,Ta,W
2×1×1 supercell
M1⟷M2

## Slide 19: Conclusions
J. Phys. Chem. Lett., 8, 755-764 (2017)
J. Phys. Chem. Lett., 9, 3470-3477 (2018)
Submitted (2018)

## Slide 20
New book on the
Computational materials discovery
is published soon
14 Chapters within 3 big Sections:
Methods for materials discovery
Functional materials
Low-dimensional materials
Ready for pre-order

## Slide 21: Acknowledgements
Thank you for your kind attention!
H.A. Zakaryan
A.R. Oganov
Z. Allahyari
A.I. Samtsevich
Yu.A. Kvashnina
C. Xie
D.V. Rybkovskiy

## Slide 22: Vickers hardness
There are 3 empirical models, which can be applied to estimate the Vickers hardness
Lyakhov-Oganov model (Phys. Rev. B. 84, 092103, 2011)
Gao model (Phys. Rev. Lett. 91, 015502, 2003)
Chen model (Intermetallics, 19, 1275, 2011)

## Slide 23
Fracture toughness could be estimated using the empirical equation developed in our lab [1]
[1] H.Niu, S.Niu, A.R. Oganov, PRL, submitted (2018)
where
Fracture toughness

## Slide 24: Vickers hardness
Chart: 
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 | 7.0 | 8.0 | 9.0 | 10.0 | 11.0 | 12.0 | 13.0 | 14.0 | 15.0 | 16.0 | 17.0
Lyakhov-Oganov model | 21.5 | 22.9 | 28.6 | 34.1 | 32.9 | 24.8 | 33.1 | 24.5 | 31.5 | 21.5 | 34.8 | 34.6 | 31.3 | 41 | 31.6 | 59.5 | 44.4
Gao's model | 28.1 | 26.2 | 32.6 | 32.9 | 36.6 | 23.6 | 25.1 | 27.3 | 26.6 | 24.8 | 35.8 | 36.8 | 31.8 | 37.9 | 46.8 | 57.2 | 46.3
Chen's model | 22.6 | 27.9 | 33.2 | 28.1 | 47.6 | 16.6 | 7.2 | 21.6 | 16.7 | 14.1 | 21.4 | 28.2 | 15 | 11 | 2.2 | 12.5 | 29.5
regions | 0 | 60 | 0 | 60
experiment | 23 | 26 | 20 | 26 | 46 | 48 | 10 | 13 | 18 | 21 | 13 | 15
theory | 46.8 | 48 | 18.3 | 20.9 | 13.2 | 45.9
Cr2B
Cr5B3
CrB
Cr3B4
CrB4
CrB2
Cr7C3
Cr2C
Cr3C2
Cr23C6
CrN
CrN
Cr2N
Cr2N
CrN4
CrN4
*CrN2
Hardness, GPa
Borides
Carbides
Nitrides
*Phys. Rev. B, 93, 214104, 2016

## Slide 25: Твердость по Виккерсу
Chart: 
| W | W4B3 | W6B5 | W8B7 | WB | W4B7 | WB2 | WB3 | WB5 | W3B2 | B | Diamond | c-BN
H_C | 14.7128 | 22.6803 | 21.695 | 19.9701 | 22.6573 | 34.3311 | 40.8128 | 30.0366 | 42.6813 | 15.2917
H_LO | 17.514 | 17.5537 | 17.5918 | 16.4383 | 20.7456 | 24.9493 | 30.8753 | 30.0798 | 22.7853 | 17.7179 | 42.955 | 98 | 60
Hv, ГПа

## Slide 26: Temperature stability. Theory
where
To take into account the temperature one needs to calculate the Gibbs free energy instead of total energy
T=300 K
Chart: 
| 0.0 | 0.428571428571429 | 0.454545454545454 | 0.466666666666667 | 0.5 | 0.636363636363636 | 0.666666666666667 | 0.75 | 1.0 | 0.833333333333333
 | 0 | -0.31755 | -0.33475 | -0.33899 | -0.35053 | -0.34449 | -0.33634 | -0.27005 | 0 | -0.15586
 | 0 | -0.31755 | -0.33475 | -0.33899 | -0.35053 | -0.34449 | -0.33634 | -0.27005 | 0
T=N K
G, eV
G, eV
Chart: 
| 0.0 | 0.428571428571429 | 0.454545454545454 | 0.466666666666667 | 0.5 | 0.636363636363636 | 0.666666666666667 | 0.75 | 1.0 | 0.833333333333333
2000K | 0 | -0.33935 | -0.36635 | -0.37242 | -0.4065 | -0.34905 | -0.34904 | -0.28451 | 0 | -0.19367
convex | 0 | -0.4065 | -0.34904 | -0.28451 | -0.19367 | 0
AHA
AHA
where
A.G. Kvashnin, et al., J. Phys. Chem. Lett., 2018, 9, pp 3470–3477

## Slide 27: Temperature dependence of mechanical properties
Elastic constants could be calculated by two different ways:
E is energy, σ is stress, η is strain.
Instead of E we need to use Gibbs free energy as:
where
…
A.G. Kvashnin, et al., J. Phys. Chem. Lett., 2018, 9, pp 3470–3477

## Slide 28: Superconductivity
Allen-Dynes equation (full)
Modified McMillan equation (short)
where
McMillan approximation cannot be apply for EPC parameters λ > 2
For large λ the fill Allen-Dynes equation should be used.
Important!

## Slide 29: Search for new Cr-N phases
As a result, the CrN, Cr2N, CrN4 phases were found. The most intensive study was devoted to the new CrN4 phases

## Slide 30: More attention to Cr-N system
[3] M.D. Aguas, A.M. Nartowski, I.P. Parkin, M. MacKenzie, and A.J. Craven, J. Mater. Chem. 8, 1875 (1998).
Exp. from [3]
Comparison of experimental XRD pattern with simulations. The Pnnm-Cr2N phase was remained structurally unresolved until now – but here we finally determine its crystal structure.
CrN4 phases are in fact high energy-density materials with polymeric nitrogen chains with 2 atoms (С2/m) and flat triangular NN3-groups (similar to NO3-groups; R3c-CrN4 is structurally similar to calcite CaCO3 and NaNO3)

## Slide 31: Stability of Cr-N phases
The stability of Cr-N phases were studied by calculating the P(T) phase diagrams. All phases remain dynamical stability (no imaginary phonon frequencies). CrN4 phases are metastable due to the positive formation energy. These phases become stable under external pressure more than 5 GPa.

## Slide 32: Stability under pressure
C2/m-CrN4 - 1.96 MJ/kg
R3c-CrN4 - 3.51 MJ/kg
TNT (trinitrotoluene) - 4.6 MJ/kg
Gunpowder 3 MJ/kg
Nitroglycerin 6.6 MJ/kg
Energy density materials