## Slide 1: Effects of the surface termination on oxygen reduction rate of cathodes for fuel cells
E. A. Kotomin, R. Merkle,
Yu. Mastrikov, J. Maier

## Slide 2
Oxygen/Proton-conducting ceramic fuel cells (PCFC)
H2O
H2
O2
H+
H+
e-
e-
H2
H2O
O2
Ba(Zr,Y)O3-x
PCFC:
* higher sion at low T
* fuel not diluted
by H2O
Ba(Zr,Y)O3-x
H2O
H2
O2
O2-
O2-
e-
e-
H2
H2O
O2
(Zr,Y)O2-x
SOFC
PCFC
 700 °C
300-600 °C

## Slide 3: (La,Sr)MnO3= LSM
one of the first SOFC cathodes
well studied (M.Liu 2007-2010; D.Morgan 2009, 2015; E.Wachsman, Watson 2016
Kuklja et al PCCP 15, 5443 (2013)
Mastrikov et al, J. Phys. Chem. C 114, 3017 (2010);
Wang J.Mat. Res. 27, (2012)
main focus was on MnO2 terminated surface as the most stable, a few studies of Sr doping
However, it was shown that Sr doping makes (La,Sr)O termination more favourable
Piskunov et al PRB 78, 121406 (2008)
Orthorhombic phase stable below 750 K (modeling defects in a cubic phase could make problems)

## Slide 4: Ultimate goals of theory: Atomistic/mechanistic details of oxygen reduction (ORR) at SOFC cathode surface, including O2 adsorption, disociation, O vacancy formation/migration on the surface/bulk; with aim to optimize cathode chemical composition Challenge: what are the rate-determining reaction stages in oxygen reduction reaction Advantage of atomistic modeling: effects on terminating plane; charge redistribution.

## Slide 5: Methods: 1. Solid state physics
Density Functional Theory
Plane Wave basis set
Generalised Gradient Approximation (Hubbard U)
Perdew Wang 91 exchange-correlation functional
Projector Augmented Wave method
Conjugate Gradient method for structure relaxation
Nudged Elastic Bands for energy barriers estimation
Bader charge analysis
Spin-polarized calculations
Slabs 7 – 15 planes with 8x surface unit cell (critically important)
Notes: 5

## Slide 6
2. Quantum chemical approach
CRYSTAL 2014 code with LCAO basis set
(re-optimised Comp Mat Sci. 29, 165 (2004)
For light atoms (O), all-electron basis set (BS) for heavy atoms (Sr, Pb,Ti and Zr), the small-core pseudopotentials
Hybrid HF-DFT functionals work very good for band gaps
Bond populations and atomic charge analysis
Well suited for single slabs without repetition along z axis
Ghost basis set on vacant sites
Notes: 6

## Slide 7: (La,Sr) (001) terminated surface
Problems: it is polar – oppositely charged
(+/-1e) LaO/MnO2 planes
Stoichiometric slabs reveal macroscopic dipole moment
To avoid macroscopic dipole moment, symmetric but nonstoichiometric slabs are used (on both sides-- LaO or MnO2) with even number of planes
Dependent on the termination, Mn oxidation state (OX) is varied, which affects Vo formation energy
Example: in LSF Vo form.enthalpy changes from 0.7 eV (Fe 4+) to 5 eV (OX < 3).
Our goal- to study these effects on ORR on (La,Sr)O termination (Kotomin et al, ECS Trans. 77 (2017), Mastrikov 2018)

## Slide 8: 2 (001) slab terminations
LaO (+1) MnO2 (-1)
MnO2 (-1) LaO (+1)
LaO (+1) MnO2 (-1)
MnO2 (-1) LaO (+1)
LaO (+1) MnO2 (-1)
MnO2 (-1) LaO (+1)
LaO (+1) MnO2 (-1)
-- Choice: either non-stoichiometry, or dipole moment

## Slide 9: Electronic charge distribution
orthorhombic (001) LMO, Sr 0%, 25%, Sr 50%
7 planes, 8x surface unit cell
bulk LMO: O (-1.27 e), Mn +1.71 e considerable Mn-O bond covalency
Variation of formal Mn oxidation state:
xSr bulk (La,Sr)O MnO2
0 +3.0 +2.67 +3.25
0.25 +3.25 +3.00 +3.44
0.5 +3.50 +3.33 +3.63

## Slide 10: Vacancies in different planes
No Sr doping

## Slide 11
Two terminations show opposite trends:
ΔE = 1.2 eV transforms into difference in surface [VO..] of 5 orders of magnitude at 1000K
in agreement with D.Morgan (PRB 2015)
for formation energy estimate, use as the
reference the bulk with the same OX!

## Slide 12: 25% Sr doping
Smaller DEVo..
Different reference energies
in the bulk!
Similar results for 50% Sr

## Slide 13: oxygen adsorption sites on AO
O(2-) adsorption in "hollow" site between 2 La, not ontop of La
Charge -1.2 e is close to bulk, unlike -0.5 e on MnO2 for O(1-)
Ads. energy 4.3 eV is much larger than 1.1 eV on MnO2
atomic:
molecular:
O-O 1.46 Å
= peroxide
La-O 2.2 Å
(bulk 2.7 Å)

## Slide 14: O2 dissociation, VO.. migration
estimated VO.. migration barriers (via subsurface jumps): 1.4-1.3-1.2 eV (Sr 0-25-50%)
Compare with 0.9 eV in bulk and 0.6 eV on MnO2
Dissociation barriers: 0.2-0.6-0.8 eV (Sr 0-25-50%)
compare ~ 1 eV on LaO La2NiO4 (Kilner 2016)
Large enough supercell is critically important
Our adsorbate coverage 12%

## Slide 15: O2 dissociation on AO
initial state = peroxide
transition state +0.60eV
next frame -0.14eV
1.90 Å
1.49 Å
2.30
2.35
2.47
2.64
2.22
2.32
2.31
2.50
2.44 Å
2.14
2.29
2.14
2.37

## Slide 16
O2
La La
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
-5.0eV
-4.3eV
incorporation
dissociation
low barrier
molecular
adsorption
1.4eV
encounter of
adsorbed O and VO..
via subsurface
LMO- LaO termination, slab with initial Mn oxidation state 2.67+
DE
2(-0.75eV)
high O- coverage
surface almost
poisoned by O-
very low surface [VO..]
10-7 relative to MnO2 termination
with same ox. state at 1000 K
 O incorporation is
rate determining step
O-O 1.46 Å
peroxide

## Slide 17
O2
La La
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
-4.0eV
-2.9eV
incorporation
dissociation
molecular
adsorption
1.3eV
encounter of
adsorbed O and VO..
via subsurface
La0.75Sr0.25MnO3 (La,Sr)O termination, slab with initial Mn oxidation state 3.0+
DE
2(-1.4eV)
0.6eV
high O- coverage
surface almost
poisoned by O-
very low surface [VO..]
10-5 relative to MnO2 termination
with same ox. state at 1000 K
 O incorporation is
rate determining step
O-O 1.46 Å
peroxide

## Slide 18
O2
La La
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
-2.5eV
-1.3eV
incorporation
dissociation
molecular
adsorption
1.2eV
encounter of
adsorbed O and VO..
via subsurface
La0.5Sr0.5MnO3 (La,Sr)O termination, slab with initial Mn oxidation state 3.3+
DE
2(-2.4eV)
moderate O- coverage
about 10-30%
still higher than on MnO2
0.8eV
dissociation barrier increases
with increasing Sr content,
 less negative overall reaction enthalpy,
less electron transfer to ads. O2
still low surface [VO..]
10-4 relative to MnO2 termination
with same ox. state at 1000 K
 O incorporation is
rate determining step
O-O 1.38 Å
superoxide

## Slide 19
Our goal is modelling of all steps of the ORR in order to find limiting one.
Entropy effects important under realistic operation conditions (1000 K).
Mastrikov et al, J. Phys. Chem. C 114, 3017 (2010); Wang J.Mat. Res. 27, 2012
MnO2 (001) termination:

## Slide 20: CONCLUSIONS
Surface termination, surface dipoles and Mn oxidation states (nonstoichiometry) play very important role in slab calculations of polar surfaces
O (O2) adsorption energy on (La,Sr)O surfaces
much larger than on MnO2 (1-2 order larger coverg.)
BUT concentrations of VO.. is 4-7 orders smaller
Thus, ORR rate at (La,Sr)O surface is much slower than on MnO2 termination
could be relevant for many similar polar surfaces

## Slide 21: Acknowledgments
Many thanks to:
E. Heifets
R. Evarestov
D.Gryaznov
R.Dovesi

## Slide 22: Joint experimental- theoretical study on BSCF-LSCF solid solution solutions
Recent review articles related to SOFC:
L. Wang et al, J.Mater. Res. 27, 2000 (2012)
M. Kuklja et al, PCCP (review) 15, 5443 (2013)
R.Catlow (ed.) Computational Approaches to Energy Materials, Wiley, 2013, Chapter 6.
Yu. Mastrikov et al, PCCP 15, 911 (2013)
D. Fuks et al, J. Mater. Chem. A1, 14320 (2013)

## Slide 23
-1.1eV
Mn O Mn
O-
O
Mn O2- Mn
O O
Mn O Mn
+0.6eV
-1.6eV
O2
Mn O Mn
O-
Mn Mn
+0.7eV
-O O-
Mn O Mn
O Mn
Mn O Mn
O-
O
O O
Mn O Mn
+0.6eV
-O O-
Mn O Mn
O Mn
+0.7eV
O-
Mn Mn
Mn O2- Mn
2(-1.5eV)
DE
DG
2(-1.5eV)
For comparison: LM (Mastrikov, 2010) MnO2 termination
dissociation
encounter of
adsorbed O and VO..
rate determining:
or

## Slide 24: Effects of LSO surface charge
AO surface charge smaller
than for MnO2
part of MnO2 surface dipole
compensated by different
surface rumpling


## Slide 25
O2
La La
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
-5.0eV
-4.3eV
incorporation
dissociation
low barrier
molecular
adsorption
1.4eV
encounter of
adsorbed O and VO..
via subsurface
LaMnO3 LaO termination, slab with initial Mn oxidation state 2.67+
DE
DG
2(-0.75eV)
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
high O- coverage
(but plateau 50%?)
surface almost
poisoned by O-
very low surface [VO..]
10-7 relative to BO2 term.
with same ox state
at 1000 K
 O incorporation is rds

## Slide 26
O2
La La
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
-4.0eV
-2.9eV
incorporation
dissociation
molecular
adsorption
1.3eV
encounter of
adsorbed O and VO..
via subsurface
La0.75Sr0.25MnO3 (La,Sr)O termination, slab with initial Mn oxidation state 3.0+
DE
DG
2(-1.4eV)
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
high O- coverage
(but plateau 50%?)
surface almost
poisoned by O-
very low surface [VO..]
10-5 relative to BO2 term.
with same ox state
at 1000 K
 O incorporation is rds
0.6eV

## Slide 27
O2
La La
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
-2.5eV
-1.3eV
incorporation
dissociation
molecular
adsorption
1.2eV
encounter of
adsorbed O and VO..
via subsurface
La0.5Sr0.5MnO3 (La,Sr)O termination, slab with initial Mn oxidation state 3.3+
DE
DG
2(-2.4eV)
La La
O-
O
La La
O O
La La La
-O O-
O-
La La
La O2- La
moderate O- coverage
(still higher than on BO2)
coverage 10-30%
still low surface [VO..]
10-4 relative to BO2 term.
with same ox state
at 1000 K
 O incorporation is rds
0.8eV
dissociation barrier increases
in parallel to less negative
overall reaction enthalpy
from LM to L5S5M

## Slide 28: Charge redistribution near surfaces
(a) xSr=0 |  |  |  |  | (b) xSr=0.50 |  |  |  | 
 | La | Mn | O | plane | La | Sr | Mn | O | plane
T |  | 1.69 | -1.20 | -0.71 |  |  | 1.77 | -1.14 | -0.51
 | 2.09 |  | -1.20 | 0.89 | 2.09 | 1.59 |  | -1.18 | 0.66
 |  | 1.83 | -1.21 | -0.59 |  |  | 1.88 | -1.16 | -0.44
Central | 2.08 |  | -1.25 | 0.83 | 2.09 | 1.57 |  | -1.25 | 0.58
Bulk | 2.09 | 1.78 | -1.25 |  | 2.10 | 1.58 | 1.85 | -1.21 | 
(a) xSr=0 |  |  |  |  | (b) xSr=0.50 |  |  |  | 
 | La | Mn | O | plane | La | Sr | Mn | O | plane
T | 1.99 |  | -1.34 | 0.64 | 2.00 | 1.57 |  | -1.33 | 0.45
 |  | 1.59 | -1.29 | -0.99 |  |  | 1.78 | -1.24 | -0.70
 | 2.07 |  | -1.30 | 0.77 | 2.09 | 1.58 |  | -1.24 | 0.60
Central |  | 1.69 | -1.27 | -0.85 |  |  | 1.78 | -1.24 | -0.70
bulk | 2.07 | -1.6 | -1.3 |  | 2.09 | 1.59 | 1.79 | -1.24 | 
Effective atomic and plane charges, MnO2 termination
(La,Sr)O termination

## Slide 29: Charge redistribution
Comparison for the same Mn oxidation state:
surface O ions more negative for AO than MnO2
(-1.34 vs -1.20 e),
La charge less positive (+1.99 vs +2.09 e)
surface MnO2 layers more covalent than bulk
(decreased Mn and O charges)

## Slide 30: Density of states for different Sr doping
(La,Sr)O
(La,Sr)O termination:
Reference: deep O 2s level
E Fermi decreases with OX (Sr content)
VB top consists of Mn t2g, eg states
overlap with O 2p
Mn ions in 2-, 4-planes close to bulk

## Slide 31: DOS vs Sr content
MnO2
MnO2 termination:
Surface Mn t2g is wider and split off
Mn ions in 3 plane close to bulk
Sr doping does not affect splitting

## Slide 32: Variation of oxygen exchange rates for MnO2 termination
.
or
Notes: 32