## Slide 1
7th School-Conference
Atomistic Simulations of Functional Materials
Center for Photochemistry of RAS
June 12-13, 2018
Correlations of Particle Motion in Supercooled Liquids
Vasily Pisarev, Elena Kirova, Dmitry Fleita,
Genri Norman

## Slide 2: Phases of Substances

## Slide 3: Extended List of “Phases”
Thermodynamically stable phases
Solid
Liquid
Gas

## Slide 4: Extended List of “Phases”
Thermodynamically stable phases
Solid
Liquid
Gas
Metastable phases
Superheated solid
Superheated liquid
Supercooled liquid
Supersaturated vapor

## Slide 5: Extended List of “Phases”
Kinetically locked states
Glass
Li Zhong et al., Nature, 512, 177 (2014):
Monoatomic metallic glasses

## Slide 6: Microscopic Definition of “Non-Thermodynamical” Phases
Thermodynamics and statistical physics point of view:
  Stable states correspond to global minima of the thermodynamic potential
  Metastable states are local minima
  Glasses are non-ergodic states (do not exist in thermodynamics)
How can we tell those states by looking at atomic-scale structure and dynamics?

## Slide 7: Outline
Overview of atomistic model
Glass transition criteria
Glass transition and shear stress autocorrelation functions (SACF)
Correlation of displacements and supercooling
Conclusions

## Slide 8: Atomistic model

## Slide 9: The Molecular Dynamics Model
Embedded atom method potential for Al (Foiles et al.,1998)
The initial conguration

## Slide 10
T, K
t
Quasi-Isobaric Cooling Process
|dT/dt| = const
1500
300
►
Cooling
Measurements
(rescaling of velocities)

## Slide 11
Glass Transition Criteria

## Slide 12
INCREASE OF VISCOSITY (1012 Pa·s)
Splitting of the second peak
of the pair correlation function (structural).
Formation of clusters
in the systems (structural).
Changes in heat capacity during cooling or heating (calorimetric).

## Slide 13: Structural Criteria
Splitting of the second peak
of the pair correlation function
Formation of
icosahedral clusters
Hypothesis: F. C. Frank, Proc. R. Soc. London A 215, 43 (1952)
Confirmation (Electron Nano-Diffraction):
A. C. Y. Liu, M. J. Neish, G. Stokol, G. A. Buckley, L. A. Smillie, M. D. de Jonge, R. T. Ott, M. J. Kramer, and L. Bourgeois, Phys. Rev. Lett. 110, 205505 (2013)

## Slide 14: The Calorimetric Criterion
Changes in heat capacity
during cooling or heating
Н(Т) is averaged over 30 MD trajectories
with the same macroscopic state
Enthalpy of the system H = U + PV ≈ U,
as Р ≈ 0

## Slide 15
м
S/Smax
Nic/ Nic,max
1000 / T

## Slide 16
2·1012 K/s
1.3·1012 K/s
6·1011 K/s

## Slide 17: Shear Stress Autocorrelation Functions (SACF) in the Glass Transition Region

## Slide 18: Viscosity calculation: Green-Kubo Relations
Shear viscosity coefficient
Where
denote ensemble-averaging
ηxz
ηxy
ηyz

## Slide 19
19
900 K
The Stress Autocorrelation Functions

## Slide 20
20
700 K
The Stress Autocorrelation Functions

## Slide 21
21
500 K
The Stress Autocorrelation Functions

## Slide 22: Viscosity Dependence on Temperature
22
|dT/dt| = 4∙1013 К/s
*Ladyanov V I et al. Phys. Chem. Liquids 52 46 (2014)
▼
Calorimetric Tg
Kinematic viscosity (cm2/s)
Tmelt

## Slide 23
23
The Stress Autocorrelation Functions
Power law
extrapolation:

## Slide 24: “Effective Exponent”
Red: ~1013 K/s
Magenta: ~1012 K/s

## Slide 25
25
“Transverse” Stress Autocorrelation Functions (XZ, YZ)
Thickness = 82 Å
Thickness = 164 Å

## Slide 26
26
“Transverse” Stress Autocorrelation Functions (XZ, YZ)
300 K
700 K
A1
A2

## Slide 27
27
Damping Dependence on Temperature

## Slide 28
28
Damping Hysteresis
Stronger damping on re-heating, hence Tglass-liq < Tliq-glass
in accordance with calorimetric Tf < Tg

## Slide 29
29
Cooling Rate Effect
Tg increases with cooling rate,
in accordance with other criteria and
relaxation glass transition models

## Slide 30: Correlation of Displacements and Supercooling

## Slide 31
31
Correlations in Microscopic Motion
r0
Δr1
Δr2

## Slide 32
32
Correlations in Aluminum Melt

## Slide 33
33
Correlations in Aluminum (Tm=925 K) and Copper (Tm= 1350 K) Melts
CC (800 ps)
Al
Cu
Tmelt
Tmelt

## Slide 34: Conclusions
We have shown the differences in dynamics of stable liquids, supercooled liquids and glasses on the examples of metallic melts
Glass shows little shear stress relaxation and signs of transverse sound
Atoms in supercooled liquids have more correlated motion than in stable liquids
Correlation between atomic displacements is almost constant above the melting temperature and grows below the melting temperature

## Slide 36: ACF time-averaging
t
t+T
t+2T
t+3T

## Slide 37
Tf

## Slide 38: Partial crystallization (12 ·1010 K/s)
Only icosahedra-coordinated atoms are shown

## Slide 39: Partial crystallization
4. – 3 ·1010 К/s
2. – 12 ·1010 К/s
3. – 6 ·1010 К/s
1. – 4 ·1013 К/s

## Slide 40: Публикации
L.N. Kolotova, G. E. Norman, and V V Pisarev.
Glass transition of aluminum melt. Molecular dynamics study
Journal of Non-Crystalline Solids 429 (2015) 98–103
E M Kirova and G E Norman.
Viscosity calculations at molecular dynamics simulations
J. Phys.: Conf. Ser. принято
Л.Н. Колотова, Г.Э. Норман, В.В. Писарев.
Стеклование переохлаждённого расплава алюминия.
Молекулярно-динамическое исследование.
Журнал физической химии. 2015. Т. 89. №5. С. 1578-1583

## Slide 41
(time-averaged)

## Slide 43: Practical use
Display manufacture
Constructing

## Slide 44
The glass–liquid transition is a transition in amorphous materials from a hard and relatively brittle "glassy" state into a molten or rubber-like state,
as the temperature is increased.
The critical cooling rate is
the limiting rate of cooling
which is too fast for crystals to form
and the material is "locked" in a glassy state.