## Slide 1: Thermally activated delayed fluorescence in organic semiconductors: a quantum chemical study
A. Freidzon
In memory of Prof. V.G. Plotnikov

## Slide 2: Electrogeneration of excitons in OLEDs
From C. Adachi, J. Adachi, High Performance TADF for OLEDs

## Slide 3
Thermally Activated Delayed Fluorescence
From C. Adachi, J. Adachi, High Performance TADF for OLEDs
W = <S1|HSO|T1>2/ΔES1-T1

## Slide 4
Thermally Activated Delayed Fluorescence

## Slide 5
Thermally Activated Delayed Fluorescence
W = <S1|HSO|T1>2/ΔES1-T1
HSO
Profit

## Slide 6: Life is more interesting though

## Slide 7: Molecular design of TADF emitters
It is argued that for small ΔES1-T1 we need spatially separated HOMO and LUMO
From C. Adachi, J. Adachi, High Performance TADF for OLEDs

## Slide 8: Molecular design of TADF emitters
However, spatially separated HOMO and LUMO lead to small transition dipole
From C. Adachi, J. Adachi, High Performance TADF for OLEDs
Donor–X–Acceptor molecules are proposed as TADF emitters
μ = <φL|r|φH>

## Slide 9
Molecular design of TADF emitters
S0
S1
T1
~kT
If both T1 and S1 are HOMO→LUMO excitations,
E(T1 )≤E(S1) over the entire PES (Hund’s rule)
HSO is small (El-Sayed’s rule)
Nonzero WTS only due to the small ΔE(S-T)
WTS ≤ WST; to avoid back-transfer, S1 should be highly emissive
which is hardly possible when HOMO and LUMO are spatially separated
A different model should be applied
Collision

## Slide 10
Molecular design of TADF emitters
Vibronic interactions are important
Using Marcus-like rate constant expression
or
l is S-T reorganization energy
ISC
RISC
Some other states should be involved
Nevertheless, the problem of low Vij remains
Vij
ΔGij

## Slide 11
Let’s look at the typical TADF molecule
Bis-carbazolyl-phthalonitrile 2CzPN
Blue emitter (473 nm)
C2 symmetry

## Slide 12
Possible low-lying excited states of 2CzPN
Triplets | Singlets
3LE(PN)
3LE(Cz)
1ICT
This work
3ICT

## Slide 13
Possible low-lying excited states of 2CzPN
This work
S0 (C2)
T1 (C2)
S1 (C2v)

## Slide 14
Energy levels of 2CzPN
1ICT
XMCQDPT2/SA(10)-CASSCF(16,12)/6-31G(d,p)//BHHLYP/6-31G(d,p)
labs(calc) = 374 nm
labs(exp) = 369 nm
Note the high density of singlet and triplet states: high probability of nonadiabatic interactions

## Slide 15
Energy levels of 2CzPN
XMCQDPT2/SA(10)-CASSCF(16,12)/6-31G(d,p)//BHHLYP/6-31G(d,p)
3LE(PN)
3LE(PN)
3LE(PN)
3LE(PN)
3ICT
1ICT
3ICT
RISC
kRISC(3ICT->1ICT) = 2.78E-03 s-1
tRISC(3ICT->1ICT) = 359 s
kRISC(3LE->1ICT) = 8.98E+01 s-1
tRISC(3LE->1ICT) = 0.01 s
ISC
kISC(1ICT->3ICT) = 6.01E+05 s-1
tISC(1ICT->3ICT) = 1.66E-06 s
kISC(1ICT->3LE) = 3.39E+07 s-1
tISC(1ICT->3LE) = 2.95E-08 s
lph(calc) = 526 nm
lph(exp) = 532 nm
kph = 2.80 s-1
tph = 0.36 s
lfl(calc) = 460 nm
lfl(exp) = 473 nm
kfl = 2.87E+04 s-1
tfl = 3.48E-05 s
kfl < kisc. What makes 2CzPN fluorescent?

## Slide 16
The role of vibrations
Lax’s model of absorption and emisson spectra
Franck—Condon Displaced Harmonic Oscillator model

## Slide 17
The role of vibrations
Non-condon effects
Antisymmetric vibrations transferring S1 to S0
Mode 7 (12.38 cm-1)
Mode 8 (28.32 cm-1)

## Slide 18
The role of vibrations
Non-Condon effects
Deformations along Modes 7 and 8 result in 2 order of magnitude decrease in the radiative lifetime of S1 state!
Deforming the molecule along 1, 2, …, 20 quanta of
Modes 7, 8, 13, and 24
The vibration periods of Modes 7 and 8 are 2.7 and 1.2 ps (much faster than all the above processes)

## Slide 19
Proposed mechanism of TADF in 2CzPN
Electrogeneration of 3LE(PN) state | 
Route to singlet emission | Competing processes
RISC to 1ICT surface with kRISC(3LE->1ICT) = 8.98E+01 s-1 and tRISC(3LE->1ICT) = 0.01 s | Phosphorescence with kph = 2.80 s-1 and tph = 0.36 s
Emission from 1ICT minimum with kfl = 2.87E+04 s-1 and tfl = 3.48E-05 s | ISC to 3ICT with kISC(1ICT->3ICT) = 6.01E+05 s-1 and tISC(1ICT->3ICT) = 1.66E-06 s and to 3LE(PN) with kISC(1ICT->3LE) = 3.39E+07 s-1 and tISC(1ICT->3LE) = 2.95E-08 s
Vibrations with n = 12.38 and 28.32 cm-1 (~1-3E-12 s) | 
Emission from vibrationally deformed 1ICT with at least 100-1000-fold rate | 

## Slide 21: Density Functional vs. Multireference Methods
Why it is important?
Correct state ordering influences nonradiative constants and energy transfer pathways in the material
kST
T1
T2
T3
T4
Too low
S1
S2
S3
Correct
kST is calculated for the wrong states!
kST
T1
T2
T3
T4
Correct
S1
S2
S3
Correct
Interacting states are correctly predicted
The problem of proper state ordering

## Slide 22
Thank you for your attention!